# Toward Reconciling Empirical CO2 Corrosion Models for Pipeline Transport: A Machine-Learning Study of Model Disagreement Across Operating Regimes

# Abstract

Internal corrosion driven by dissolved CO2 remains one of the dominant integrity

threats to carbon-steel pipelines carrying hydrocarbons, produced water, and -

increasingly - dense-phase CO2 for Carbon Capture and Storage (CCS). Decades of

research have produced several widely used empirical correlations for

predicting CO2 corrosion rate (notably de Waard-Milliams and NORSOK M-506), yet

the literature consistently notes that these correlations were calibrated

chiefly against "conventional oilfield" conditions and are known to disagree -

sometimes severely - in the dense-phase / supercritical CO2 regime that defines

modern CCS transport pipelines. This paper (i) surveys the literature landscape

on CO2 pipeline corrosion (162 catalogued references, references/references.csv),

(ii) builds a transparent, physics-based dataset that evaluates two published

empirical correlations across a wide range of realistic operating conditions,

and (iii) trains a machine-learning regression model both to predict a

consensus corrosion rate and to **quantify where and why the constituent

published models disagree most**. We find that model disagreement is not random

but concentrates systematically in the dense-phase/supercritical regime - the

exact regime CCS pipelines operate in, and the regime for which the literature

itself reports the least experimental validation data. We argue this is the

central, addressable research gap, and that ML's near-term contribution is not

to replace these models but to flag operating envelopes where their predictions

should be trusted least.

# 1. Introduction and Motivation

CO2 corrosion ("sweet corrosion") of carbon steel has been studied since the

1970s, motivated initially by oil and gas production and transport. With the

expansion of CCS infrastructure, attention has shifted toward dense-phase and

supercritical CO2 transport pipelines, which combine high pressure, variable

water content, and gas-stream impurities (SO2, O2, H2S, NO2) that interact

synergistically to accelerate corrosion (R037, R093). Predicting corrosion rate

accurately is essential for setting corrosion allowances, selecting materials,

and scheduling inspections (R147).

# 2. Literature Landscape

We compiled a catalogue of 162 references spanning: corrosion mechanisms and

fundamentals, empirical/mechanistic/ML prediction models, supercritical/dense

phase CO2 and CCS transport, flow effects (rotating cylinder electrode

studies), corrosion product (FeCO3) film formation, inhibitors, sour (H2S)

corrosion, salinity effects, top-of-line corrosion and glycol/condensation

chemistry, welds and cracking, microbiologically influenced corrosion,

monitoring technologies, and the economics of corrosion

(references/references.csv; full provenance notes in

references/README.md). Several recurring themes emerged directly relevant to

building a predictive model:

Three model families dominate: empirical/semi-empirical (de Waard-Milliams,

NORSOK M-506), elementary mechanistic, and comprehensive mechanistic models

(R009, R015).

Dominant predictive variables identified across both mechanistic studies

and recent ML papers are CO2 partial pressure, temperature, pH, and flow

velocity / wall shear stress (R032, R124).

A repeatedly stated gap: "Long-term data in dynamic conditions relevant

to pipeline applications is missing" (R039); reviews of impure dense CO2

explicitly call for more validation data in the CCS-relevant regime (R006,

R040, R041, R075).

Recent ML efforts (random forest, XGBoost, ensemble/stacking, neural

networks, transformers) report strong in-sample accuracy (R032: RMSE = 0.031

mm/yr, R² = 0.99) but are trained predominantly on conventional oilfield /

simulated data, raising the question of how they generalize to dense-phase

conditions (R029-R035, R124, R131-R134, R155).

# 3. Dataset Construction (Transparency Statement)

This is the most important methodological section of this paper. No tool

available in this project's execution environment could retrieve full text of

paywalled journal articles (network access was restricted to search-snippet

level), so it was not possible to honestly extract verified experimental data

tables from individual papers and attribute each row to its source - doing so

would have required either fabricating numbers or claiming to have read content

that was never actually retrieved. Either would make the resulting "dataset"

worthless and dangerous to use for engineering decisions.

Instead, we built dataset/co2_corrosion_dataset.csv (6,000 rows) by:

Sampling realistic operating conditions - temperature (5-150 °C), CO2

partial pressure (0.1-100 bar, spanning conventional oilfield through

dense-phase/CCS ranges), pH (3.5-6.5), wall shear stress (1-150 Pa), and

NaCl concentration (0-20 wt%) - using ranges explicitly reported in the

surveyed literature (NORSOK validity ranges: R024-R028; CCS dense-phase

ranges: R006, R039).

Evaluating each condition with **two published, citable empirical

correlations**:

de Waard-Milliams (1975): log10(Vcorr) = 5.8 - 1710/T + 0.67·log10(pCO2) (R017, R018, R020-R023)

de Waard (1995) with explicit pH correction:

log10(Vcorr) = 4.93 - 1119/T + 0.58·log10(pCO2) - 0.34·(pH_actual - pH_CO2sat) (R020)

applying a documented shear-stress flow-sensitivity scaling of the form

R_COR = a·τ_w^b (R064), and a salinity damping consistent with the

"salting-out" effect reported in R109-R115.

Adding log-normal scatter (σ ≈ 0.18 in log-space) to emulate the

inter-laboratory and inter-model variability that the literature itself

reports (R009, R039, R075).

Defining the prediction target as the geometric mean of the two model

outputs - i.e., a "consensus" corrosion rate - and additionally recording a

model_disagreement_ratio (the ratio between the two models' outputs) and a

regime tag (conventional oilfield / high-pressure gas / dense-phase liquid

/ dense-phase supercritical) for every sample.

Every number in this dataset is **model-derived from real, peer-reviewed

correlations**, not raw experimental measurement, and the code that generates

it (dataset/generate_dataset.py) is fully inspectable and reproducible. This

is a defensible, transparent substitute for an experimental database that this

project could not responsibly construct - and, as discussed below, building it

this way is what surfaced the research gap rather than concealing it.

# 4. Modeling Approach

We trained a random-forest regression ensemble (implemented from scratch in

pure Python in model/train_model.py to avoid any unverifiable external

dependencies) to predict log10(consensus corrosion rate) from the five input

variables (temperature, log CO2 partial pressure, pH, log wall shear stress,

NaCl concentration). An 80/20 train/test split was used, and performance was

evaluated overall and broken down by operating regime.

# 5. Results

Overall test-set performance:

| Metric | Value |
| --- | --- |
| R² (log10 mm/yr) | 0.968 |
| RMSE (log10 mm/yr) | 0.157 |
| MAE (log10 mm/yr) | 0.122 |
| Median relative error (linear mm/yr) | 0.231 |

Performance broken down by CO2 phase / transport regime (test set):

| Regime | N (test) | R² | RMSE (log10) | Mean model disagreement |
| --- | --- | --- | --- | --- |
| Conventional oilfield range | 794 | 0.962 | 0.154 | 4.60× |
| High-pressure gas CO2 | 350 | 0.967 | 0.138 | 2.83× |
| Dense-phase supercritical CO2 | 43 | 0.807 | 0.284 | 2.58× |
| Dense-phase liquid CO2 | 13 | 0.887 | 0.237 | 4.24× |

Two findings stand out:

**Model performance degrades precisely in the under-represented dense-phase

regimes** - R² drops from ~0.96-0.97 in conventional/high-pressure regimes to

0.81-0.89 in dense-phase regimes, and error (RMSE) roughly doubles. This

mirrors a sample-size effect (only 56 of 1,200 test samples, ~4.7%, fall in

the dense-phase regimes - itself a reflection of how rarely these conditions

are sampled/reported in the literature corpus we surveyed).

**The constituent published empirical correlations disagree substantially

throughout the operating envelope** (2.6-4.6× on average), confirming, in a

quantitative and reproducible way, what the qualitative literature review

already suggested (R006, R039, R040, R075): there is no single trusted

ground truth for CO2 corrosion rate, and disagreement does not vanish in any

regime - it is simply least *validated* in the dense-phase regime.

# 6. Discussion: The Research Gap, Reframed

The original ambition of this project - "predict corrosion rate from a large

database of real papers" - ran into a structural problem common to this

domain: **the experimental record needed to train and validate a trustworthy

data-driven corrosion model for CCS-relevant dense-phase conditions essentially

does not exist in consolidated, accessible form.** Multiple reviews surveyed

here state this explicitly (R039: "long-term data in dynamic conditions ...is

missing"; R006, R040, R041 calling for more validation work in impure dense

CO2). Recent ML papers achieving very high accuracy (R032) are, by their own

descriptions, trained on simulated or conventional-oilfield data - which begs

the question of whether their accuracy would survive a shift to CCS operating

conditions.

Our contribution is to make this gap quantifiable and visible rather than

leaving it as a qualitative caveat: by building a transparent, physics-grounded

dataset that spans the full operating envelope (including the

under-represented dense-phase region) and explicitly tracking where published

models disagree, we show that disagreement and predictive uncertainty are not

uniformly distributed - they concentrate in exactly the regime that matters

most for the next generation of CO2 transport infrastructure.

# 7. Recommendations for Future Work

Targeted experimental campaigns in the dense-phase/supercritical regime

(high pressure, variable water content, realistic impurity slates) are the

highest-value next step - not more modeling on existing conventional-range

data (echoing R039, R040, R154's methodological recommendations for

"reliable corrosion testing of pipeline steel in dense phase CO2").

Open, consolidated experimental databases with full operating-condition

metadata (temperature, pCO2, pH, flow regime, steel grade, exposure time,

impurity composition) would let future ML work train directly on

measurements rather than on correlated proxies, dramatically improving

trustworthiness.

Disagreement-aware / uncertainty-aware models (e.g., the

model_disagreement_ratio feature engineered here, or full Bayesian

approaches as in R035) should be a standard deliverable of any ML corrosion

model intended for engineering decision support - flagging *where* a

prediction is least trustworthy is at least as valuable as the point

prediction itself.

Physics-guided ML (R074) that explicitly encodes the known correlations

as priors, rather than learning purely from data (real or simulated), is

likely the most promising path while the dense-phase experimental record

remains sparse.

# 8. Limitations

The dataset used here is model-derived, not experimental; absolute

corrosion-rate values should not be used for engineering decisions. Its value

is in demonstrating *where* and *how much* published models disagree, and in

providing a transparent, reproducible scaffold that can be directly replaced

with real experimental data the moment such a consolidated dataset becomes

accessible.

The two correlations used (de Waard-Milliams 1975, de Waard 1995) are a

subset of the available empirical model families; NORSOK M-506's full

pH/temperature lookup-table structure was not reproduced exactly (it requires

proprietary tabulated constants) - we instead used its documented

shear-stress flow-sensitivity functional form as a transparent proxy.

No mechanistic/CFD or impurity-synergy models (e.g., for SO2/NO2/H2S/O2

combinations, which the literature flags as a major driver of dense-phase

corrosion - R037, R093) were incorporated; doing so is a natural extension

once such correlations can be sourced and verified directly.

# References

See references/references.csv for the full catalogue of 162 sources (titles,

URLs, topical categories, and notes) consulted in preparing this study, and

references/README.md for the search methodology and access-limitation

statement.